## Slide 1: Designing Biomimetic Twisted Polymer Torsional Actuators
Heidi P. Feigenbaum, Associate Professor, Northern Arizona University
Michael W. Shafer, Assistant Professor, Northern Arizona University
Diego R. Higueras Ruiz, M.S. Candidate, Northern Arizona University
Amy Swartz, M.S. Candidate, Northern Arizona University
SMASIS 2017, Snowbird, UT, USA, September 19, 2017

## Slide 2: Twisted Polymer Actuators
Drawn Polymer Monofilaments: Fishing line
  Extremely inexpensive
Twisted Polymer Actuators (TPAs)
  Anneal twisted drawn polymer monofilaments
Straight-Twisted Polymer Actuators (STPAs)
  Torsional actuation
Twisted Coiled Polymer Actuators (TCPAs)
  Linear actuation

## Slide 3: Previous Work
TCPAs have striking performance characteristics
  Specific load capacity higher than human muscle [Haines et al. 2014]
  Low actuation hysteresis [Haines et al. 2014]
  Low creep (~1.5% ) over 1.2 million cycles [Haines et al. 2014]
Similarly impressive performance of STPAs in torsion
STPAs building blocks of TCPAs
[Haines et al. 2014]

## Slide 4: This Work
Designing STPAs
Actuation process of STPAs
Testing torsional STPAs
  Two configuration
Review models for the themal behavior of STPAs
Measuring thermal expansion
  Key part of models and actuation process
Predicting torsional actution of STPAs

## Slide 5: Mechanics of STPAs
Precursor Fiber
(monofilament)
Straight-twisted polymer actuator (STPA)
Twist under tensile load. Thermally anneal.
ΔT
High stiffness polymer chain now wraps around larger circumference causing shear deformation.
ΔT
Heated precursor fiber radially expands
Amorphous
Crystallite
Interfibrillar
tie chains
Prevorsek microstructural model

## Slide 6: Testing STPAs
Configuration 1 – single monofilament of STPA
  Simpler
Configuration 2 – 3 parallel STPAs gently twisted together (like rope)
  Larger loads
  Potential for heating wire core
  The twisting together must be gentle or else create a linear actuator
Nylon 6 - Berkley Trilene Big GameTM 80lb monofilament
All materials used were desiccated

## Slide 7: Experimental Methods

## Slide 8: Experimental Results
Config. 1 – single STPA
Config. 2 – parallel
Pre-load per cross-sectional area equivalent for the two designs
More torsional stroke with parallel configuration
Notice the first cycle effect
Nearly full recovery after first few cycles
Notes: Shows actuation behavior. But ideally for design you want to be able to model and optimize the configuration. To do that you need a model!

## Slide 9: Aziz et al. [2016] Model for STPAs
1D and does not account for length change of fiber or STPA
  Where is untwist of STPA, is radial thermal expansion of twisted samples, is initial twist in the STPA
Can include mechanical load, but requires measurement of material properties on twisted samples, so need to re-measure for each inserted twist.
Before heating
After heating
Type equation here.
Fiber length
Fiber length

## Slide 10: Shafer et al. [2016] Model for STPAs
2D & accounts for length change
  where is axial thermal expansion of precursor monofilament, is radial thermal expansion of precursor monofilament
Properties of untwisted fibers properly transformed
Because different twist at each radius, different predictions at every radial position

## Slide 11: Calibration of Models
Aziz et al.
  Initial twist of STPA
  Radial expansion of twisted
Shafer et al.
  Initial twist, radius, and length of STPA
  Radial and axial thermal expansion of untwisted monofilament
Axial Thermal Expansion

## Slide 12: Radial Thermal Expansion
Displacement in oil baths
  Multiple fibers in graduate cylinder
    Measure volume change & subtract axial expansion
    Resolution poor
  Single fiber in capillary tube
    Issue with bubbles
    Suggest water release
Vapor bubble migration in sample
T = 20 C
T = 100 C
Capillary Test Results
T = 20 C
T ~ 100 C
 Need to control for humidity! We desiccate samples.

## Slide 13: New Method for Radial Expansion
Keyence Digital Microscope under 300x magnification
Samples
  All desiccated
  All cut into slices ~0.5 mm thick using a microtome
  Untwisted & Twisted
  Some stretch during annealing (pre-strained)
  Some thermally pre-cycled
The distance between two arbitrary points was tracked over the temperature range and used to calculate radial thermal strain.
30ºC
41ºC

## Slide 14: Radial Thermal Expansion Results
Highly repeatable radial thermal strains
Results nearly the same with and without twist
Results nearly the same with and without pre-strain
Nearly full recovery & minimal hysteresis after thermally pre-cycled
No thermal pre-cycle
Thermally pre-cycle

## Slide 15: Predicting Free Torsion

## Slide 16: Conclusions & Future Work
Much promise for use of TPAs
Need to control humidity
  We use desiccated samples
Need to pre-cycle before use
  First few cycles actuate differently than all subsequent cycles
  Radial thermal expansion fully recovers with minimal hysteresis if thermally pre-cycle
Radially thermal expansion independent of twist and pre-strain
Shafer et al. [2016] model predicts free torsion reasonably well
Future Work:
Modeling STPAs with thermal and mechanical loading using precursor properties
  Predict actuation results
  Design initial twist
Modeling of TCPAs

## Slide 17: Thank you for your attention!
Questions?

## Slide 18: TPA Fabrication & Actuation Processes
Precursor Fiber
(monofilament)
Straight-twisted polymer actuator (STPA)
Twisted-coiled Polymer Actuator (TCPA)
Contraction
Twist & anneal
ΔT
High stiffness polymer chain now wraps around larger circumference causing shear stress and deformation due to low shear stiffness.
ΔT
Twist/coil & anneal.
ΔT
Fabrication
Actuation
Torsional response of STPA translates to contraction of TCPA.
Precursor fibers expand radially (and contract axially – not shown) when heated

## Slide 19: Asymmetric thermal expansion
Actuation thought to be driven by asymmetric thermal expansion
Asymmetric thermal expansion thought to be driven by the microstructure [Prevorsek et al. 1973, Bruno et al. 1998]
Inter-fibril tie chains vibrate mainly radially  radial expansion & axial contraction
Amorphous
Crystalline
Inter-fibril tie chain

## Slide 20: Modeling the thermal behavior of STPAs
Before Heating
After Heating
Type equation here.
Fiber length
Fiber length

## Slide 21
[Aziz et al. 2016]

## Slide 22: Experimental Results